The governing standard for Stainless Steel (SS) valves is still ASME B16.34, but they are governed by specific Material Groups within that standard to account for the unique pressure-temperature ratings of stainless alloys.

While carbon steel follows Material Group 1, stainless steel valves follow Material Group 2.

Material Specifications (ASME Section II / ASTM)

ASME B16.34 relies on specific material standards to define the grade of stainless steel used for the valve body:

- Cast Stainless Valves: Governed by ASTM A351 / ASME SA351 (e.g., Grade CF8 for 304SS, Grade CF8M for 316SS).

- Forged Stainless Valves: Governed by ASTM A182 / ASME SA182 (e.g., Grade F304, Grade F316).

Material Groups inside ASME B16.34

The pressure-temperature rating tables change depending on the exact stainless alloy:

- Group 2.1: Standard 304 and 316 stainless steel.

- Group 2.2: 304L and 316L (Low-carbon variants used to prevent sensitization during welding, which have lower pressure ratings at high temperatures).

- Group 2.4 / 2.5: High-alloy or duplex stainless steels (e.g., UNS S31803) used for extreme corrosion resistance.

Specialized Stainless Steel Standards

Depending on the application, stainless steel valves must comply with additional supplementary codes:

- API 603 (Corrosion-Resistant Valves): This standard modifies ASME B16.34 specifically for stainless steel gate, globe, and check valves used in low-pressure, highly corrosive process piping (Class 150, 300, and 600).

- NACE MR0175 / ISO 15156: Dictates hardness limits and material processing rules for stainless steel valves used in sour gas (H2S) environments to prevent sulfide stress cracking.

- NACE MR0103: Focuses on downstream refinery sour environments for stainless alloys.

To look up the exact pressure rating or thickness, tell me:

- What is the exact grade of stainless steel (e.g., 316, 316L, Duplex)?

- What is the pressure class of your system (e.g., Class 150, Class 300)?

I can pull up the maximum allowable pressure or temperature limits for that configuration.